SECTION 07210

BATT INSULATION SYSTEM

PART 1 GENERAL

1.1 QUALITY ASSURANCE

PART 2 PRODUCTS

2.1 MATERIALS

PART 3 EXECUTION

3.1 EXAMINATION

3.2 PREPERATION

3.3 INSTALLATION

3.4 PROTECTION

# GENERAL

## QUALITY ASSURANCE

#### Insulation reference standards:

UL requirements.

ASTM-C518.

ASTM-C739.

ASTM-E84.

ASTM-E90.

ASTM-E119.

ASTM-E970.

#### Insulation value exterior walls: RSI/m-3.5 R-14.

- Insulation value exterior walls: RSI/m-1.8 R-10.

- Certification of minimum 20 percent recovered material content in fiberglass insulation.

- Certification of minimum 9 percent recovered material content in rigid plastic foams.

- Certification of minimum 75 percent recovered material content in cellulose insulation.

# PRODUCTS

## MATERIALS

#### Insulation, spandrel:

Mineral wool fibers and resinous binders formed into batts with aluminum foil scrim/vapor retarder.

#### Vapor retarder:

Two directional, reinforced, foil faced vapor retarder or foil/mylar.

Permeance: Not exceeding 1.15 ng/Pasm2 0.02 perm.

ASTM-E84 flame spread: 25 maximum.

Rolls: 1270 mm 50 IN wide.

Base: Sisalkraft Pyro-Kure 615.

Optional: Alumiseal Zero Perm.

#### Vapor retarder tape:

Heavy duty 75 mm 3 IN wide laminate consisting of 0.009 mm 0.00035 IN aluminum foil, glass fiber reinforced two directional patterned Kraft paper or aluminum/mylar.

UL listed class A.

Base: FasTape 0820 FR-FSK, or FasTape 0821FR-FSK-30.

If vapor retarder tape fails to adhere to surface, spray on Norton; Spray Trim Adhesive, No.82130-1 or a similar product by 3M to augment adhesion of tape.

Specifier:  Where vapor retarder abuts steel structure with fireproofing, or curtainwall system sheet metal vapor retarder may be required.  Indicate size on exterior detail or specify.

- Sheet metal vapor retarder:

- Minimum 0.6 mm 24 GA galvanized steel bent angle; size as required.

- Provide where vapor retarder abuts steel structure.

- Provide where vapor retarder abuts curtainwall.

Specifier:  This is a system to use on masonry or concrete walls where you want insulation with minimum loss of space in room.  Foam insulation is adhered to wall and stud strips (which look like mini-floor runners for GYPSUM WALLBOARD) are embedded into foam with fasteners shot thru them to hold insulation in space and to give surface to screw GYPSUM WALLBOARD to.  Verify insulation thickness for R value. TGIF system (subparagraph 5) gives better vapor transmission factor.  If electrical outlets are required in these walls, make sure electrical uses shallow boxes.

Specifier:  Add mechanical fasteners and mastic if required. Normally only used with precast and non-rigid insulations. Could be used in stud walls, but normally not.

- Mechanical fasteners:

- Pronged hangers and slotted washers or arrow pointed hangers.

- Sized to fit insulation thickness.

- Base: GEMCO (Goodloe E. Moore,); Gemco pronged hanger with WP washer.

- Optional: Stic-Klip Manufacturing.

- Mastic for use with mechanical fasteners: GEMCO (Goodloe E. Moore.)

Specifier:  ASTM-C516, Type II, Grade-0.  Primary usage is for waterproofing backside of precast, add if you have precast.

- Waterproof coating:

- Cement base, aggregate type.

- Harris Specialty Chemical, Thoro System Products, Thoroseal containing "Acryl 60".

# EXECUTION

## Examination

#### Verify that conditions conform to requirements of Contract documents.

#### Verify that related work to be performed within indicated spaces before installation of insulation has been completed.

#### Verify that substrates are in satisfactory condition to receive insulation.

#### Do not proceed until unsatisfactory conditions have been corrected.

## Preparation

#### Clean substrates of any substances which might damage materials to be installed.

#### Remove harmful projections capable of puncturing vapor retarder.

## Installation

#### Do not install insulation which is damaged, wet, soiled, or which has been covered at any time with ice or snow.

#### Comply with insulation manufacturer’s recommendations and installation sequence.

#### Install materials in a manner which will maximize continuity of thermal envelope.  Use a single layer of insulation wherever possible to achieve indicated requirements, unless otherwise indicated.

#### Insulation Blankets/Batts:

Install properly per manufacturer’s recommendations.

Cut insulation neatly as required to fit tightly around obstructions.

Place insulation with facing oriented toward warm side of construction, unless otherwise indicated.

Tape seal joints in facing with vinyl tape.

#### Vapor Retarder:

Install vapor retarder in a manner which will maximize protection against vapor transmission.

Install vapor retarder on warm side of insulation unless otherwise indicated.

Seal overlapping joints, butt joints, and fastener penetrations.

Tape seal joints with white vinyl tape.

## Protection

#### Protect installed materials from damage until permanent concealing work is completed.

#### Where concealing work is not performed immediately after installation work of this section is completed, erect suitable temporary coverings or enclosures to prevent damage.