SECTION 06100

ROUGH CARPENTRY

PART 1 GENERAL

1.1 REFERENCE DOCUMENTS

1.2 REGULATORY REQUIREMENTS

1.3 SOURCE QUALITY CONTROL

1.4 PRODUCT DELIVERY AND STORAGE

PART 2 PRODUCTS

2.1 LUMBER

2.2 PANEL PRODUCTS

2.3 FASTENING DEVICES AND HARDWARE

2.4 ANCILLARY MATERIALS

2.5 PRESSURE PERSERVATIVE TREATED WOOD

PART 3 EXECUTION

3.1 APPLICATION OF SURFACE APPLIED WOOD PERSERVATIVE

3.2 ERECTION OF FRAMING MEMBERS

3.3 BUILDING IN OF POLYETHYLENE SHEET

3.4 WOOD FURRING AND BLOCKING

# General

## Reference documents

#### CSA O80 Series – 97,  Wood Preservation.

#### CAN/CSA O141 - 91 (R1999),  Softwood Lumber.

#### CSA O151 - M1978 (R1998),  Canadian Softwood Plywood

#### National Lumber Grading Authority (NLGA), Standard Grading Rules for Canadian Lumber, Latest edition.

## REGULATORY REQUIREMENTS

#### Comply with applicable requirements of British Columbia Building Code (BCBC).

## SOURCE QUALITY CONTROL

#### Supply lumber graded and stamped by an agency certified by Canadian Lumber Standards Administrative Board.

#### Supply plywood graded and stamped in accordance with applicable CSA standards.

## PRODUCT DELIVERY AND STORAGE

#### Protect materials from weather upon delivery to job site.

#### Store materials on raised supports.  Cover materials with waterproof covering.  Provide adequate air circulation and ventilation.

#### Do not store seasoned materials in wet or damp areas.

# Products

## LUMBER

#### Lumber:  to CAN/CSA 0141, softwood, S-P-F, S4S, surface-dry, graded and stamped in accordance with current National Lumber Grades Authority (NLGA) Standard Grading Rules for Canadian Lumber.

#### Moisture Content:  maximum 19% at time of installation.

#### Finger jointed lumber is not acceptable.

#### Framing and Board Lumber: in accordance with BCBC and as specified in schedules.

## PANEL Products

#### Douglas Fir Plywood: to CSA 0121.

## FASTENING DEVICES AND HARDWARE

#### Nails and Spikes:

#### Use common spiral nails and spiral spikes except where indicated otherwise.

#### Use hot dip galvanized finished steel for exposed exterior work, highly humid interior areas and for pressure - preservative and fire-retardant treated lumber.

## ANCILLARY MATERIALS

#### Polyethylene Film: to CAN/CGSB-51.34-M86, 100 micrometre thick.

## PRESSURE PRESERVATIVE TREATED WOOD

#### Pressure Preservative Treated Wood:  in accordance with CSA O80 Series.

# Execution

## APPLICATION OF SURFACE APPLIED WOOD PRESERVATIVE

#### Re-treat surfaces exposed by cutting, trimming or boring with liberal brush application of surface applied wood preservative before installation.

## ERECTION OF FRAMING MEMBERS

#### Install members true to line, levels and elevations.  Space uniformly.

#### Construct continuous members from pieces of longest practicable length.

#### Install blocking to facilitate installation of finishing materials, fixtures, specialty items and trim.

## BUILDING IN OF POLYETHYLENE SHEET

#### Build in sheet polyethylene in framing where framing interrupts sheet polyethylene vapour retarder specified in Section 07192, at the following locations:

#### Between top and cap plates of walls.  Leave minimum of 100 mm of sheet polyethylene on each side of interior walls and inside face of exterior walls.

#### Use sealing tape to seal joints.

## WOOD FURRING AND BLOCKING

#### Provide wood furring and blocking at locations indicated on drawings and as specified.

#### wall sheathing

#### Install wall sheathing in accordance with requirements of the British Columbia Building Code.